Assessment of Four Artificial Methods for Aging Plastic Mulch Films According to Efficiency, Rate, and Similarity to Natural Field-Aged Plastics in North Wales, UK

# Summary

This dataset was generated based on a 20-week laboratory experiment, comparing 4 artificial degradation methods to naturally weather plastic mulch films and ranking them according to their efficiency, rate, and similarity. Artificial degradation is often used to recreate and accelerate the natural aging of plastic for small-scaled simulation experiments assessing their environmental impact. However, current artificial aging methods are rarely compared against reference materials or validated using field-aged samples, creating uncertainties when extrapolating results to naturally aged plastics, making it difficult to place findings in an environmentally applicable context. Therefore, here we compared four accessible, cost-effective, and easily replicable methods (heat, UVA, and UVC irradiance at two intensities) to produce artificially degraded materials. The artificial aging methods were assessed over a duration of 5 months against degradation rate, efficiency, and similarity to field-aged samples of conventional and biodegradable plastic mulch film over a 6-month field exposure period. We utilised attenuated total reflectance-Fourier transform infrared spectroscopy to calculate the carbonyl index and measure chemical changes of the mulch film surface, as well as differential scanning calorimetry and thermogravimetric analysis. Physical changes were assessed by thickness and surface roughness measurements. We found that UVA was the most suitable and realistic artificial degradation method at a medium rate, whilst UVC is recommended for rapid degradation without the need to simulate realistic changes, and heat for processing large volumes of samples without a requirement for realistic degradation over a prolonged time period. However, the methods compared in this study yielded differential results depending on polymer type and parameter of interest. We therefore recommend establishing the degradation aim, identifying the spectral region of interest, and accounting for different polymer types to select the most appropriate method.

We recorded the following data:

- FTIR spectra of LDPE and PLA/PBAT plastic mulch films

- DSC and TGA curves for LDPE and PLA/PBAT plastic mulch films

- Film thickness and surface roughness of LPDE and PLA/PBAT mulch films

# File format

All files are in .csv format.

# File names and/or naming convention

List the file names of the data files (including the file extension).

| File name | File content |
| --- | --- |
| BioSpectra.csv | FTIR spectra of PLA/PBAT mulch film |
| LDPESpectra.csv | FTIR spectra of LDPE mulch film |
| DSCbio.csv | DSC data of PLA/PBAT mulch film |
| DSCldpe.csv | DSC data of LDPE mulch film |
| TGAbio.csv | TGA data of PLA/PBAT mulch film |
| TGAldpe.csv | TGA data of LDPE mulch film |
| PlasticProperties.csv | Film thickness and surface roughness of LDPE and PLA/PBAt mulch films |

# Nature and units of recorded values

Include information about the structure of the data (variable name(s), description, units).

Table 1. Description of variables in BioSpectra.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Method | Exposure method | n/a |
| Time | Exposure time in weeks or months | n/a |
| 656-3992 | Column headers are the wavenumber intervals (cm-1), and values for each sample are expressed in absorbance (0-1) | n/a |

Table 2. Description of variables in LDPESpectra.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Method | Exposure method | n/a |
| Time | Exposure time in weeks or months | n/a |
| 656-3992 | Column headers are the wavenumber intervals (cm-1), and values for each sample are expressed in absorbance (0-1) | n/a |

Table 3. Description of variables in DSCbio.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Treatment | Exposure method. Data provided only for end-points (i.e. 20 weeks or 6 months) | n/a |
| 25-799.833 | Column headers are the temperature (°C) and values for each temperature are expressed as heat flux (W/g) | n/a |

Table 4. Description of variables in DSCldpe.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Treatment | Exposure method. Data provided only for end-points (i.e. 20 weeks or 6 months) | n/a |
| 25-799.833 | Column headers are the temperature (°C) and values for each temperature are expressed as heat flux (W/g) | n/a |

Table 5. Description of variables in TGAbio.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Treatment | Exposure method. Data provided only for end-points (i.e. 20 weeks or 6 months) | n/a |
| 25-799.833 | Column headers are the temperature (°C) and values for each temperature are expressed as weight loss (%) | n/a |

Table 6. Description of variables in TGAldpe.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Treatment | Exposure method. Data provided only for end-points (i.e. 20 weeks or 6 months) | n/a |
| 25-799.833 | Column headers are the temperature (°C) and values for each temperature are expressed as weight loss (%) | n/a |

Table 7. Description of variables in BioSpectra.csv

| Variable/Column header | Description | Units |
| --- | --- | --- |
| Plastic | Plastic mulch film type | n/a |
| Time | Exposure time in weeks or months | n/a |
| Thickness | Film thickness | µm |
| Roughness | Film surface roughness | µm |

# Spatial coverage
[CONDITIONAL – Required for spatial data resources]

The plastic mulch films used a naturally exposed reference material were exposed at the Henfaes Research Centre, Abergwyngregyn, North Wales, UK.

# Temporal coverage and resolution
[CONDITIONAL – Required if applicable]

The field exposure period for mulch films was 6 months and lasted from 31/05/2022 – 28/11/2022.

The exposure of mulch films to artificial laboratory methods lasted 20 weeks and took place from September 2022 – March 2023.

- FTIR spectra of LDPE and PLA/PBAT plastic mulch films – field samples were measured at monthly intervals, laboratory samples were measured at weekly intervals

- DSC and TGA curves for LDPE and PLA/PBAT plastic mulch films – measured at the end points for each plastic type and exposure method (i.e. 6 months for field, and 20 weeks for artificial methods)

- Film thickness and surface roughness of LPDE and PLA/PBAT mulch films - measured at the end points for each plastic type and exposure method (i.e. 6 months for field, and 20 weeks for artificial methods)

# Collection/Generation/Transformation methods

Describe how the data were collected/generated, and if applicable how they were transformed, this can include the following details:

- Film thickness: Measured with a thickness gauge. Data recorded in paper notebook, transferred to Excel file, then exported as csv file.

- Film surface roughness: Measured with a surface roughness tester. Data recorded in paper notebook, transferred to Excel file, then exported as csv file.

- Chemical spectra (FTIR): Data was recorded using Cary 630 (Agilent) ATR-FTIR, exported as individual spectra csv files. Data was then combined for each plastic type.

- DSC/TGA: Data exported as Excel file from the instrument software, then exported as csv file.

# Experimental design/sampling regime
[CONDITIONAL - required for monitoring/experimental data]

The two mulch film types used were a conventional LDPE (Gro-Clean, GroMax, Suffolk, UK; colour: black; thickness: 23 μm) and a biodegradable PLA/PBAT (ratio 85% PBAT; 15% PLA with a polybutylene sebacate adhesive; Gro-Clean Bio-Mulch, GroMax, Suffolk, UK; colour: black; thickness: 10.5 μm) film. Organic co-contaminants were identified using a sequential solvent extraction followed by gas chromatography (GC) and GC/MS (mass spectrometry) analyses, and fillers and metals were identified by analysing the ash content of the mulch films using total reflection X-rays fluorescence (Reay et al., under review). Both mulch film types showed a high filler and metal content compared to their corresponding additive content. The most abundant additive groups for LDPE were lubricants > antioxidants > plasticisers, alongside non- intentionally added substances (e.g. ethoxylated amines as degradation products of antistatic agents). For PLA/PBAT, the most abundant additives were plasticisers > lubricants > chain extenders > antioxidants. Similar to LDPE, there were non-intentionally added substances, dominated by cyclic oligomers derived from the polymer itself, and degradation of additives beyond the analytical window (e.g. pentaerythritol fatty acid esters).

The study site for realistic field degradation was an arable field located at the Henfaes Research Centre, Abergwyngregyn, North Wales, UK (53°14’20’’N, 4°00’55’’W). The site has a temperate oceanic climate, and environmental data regarding air temperature, precipitation, solar radiation, wind speed, and relative humidity were recorded in 30-minute intervals by a meteorological station on site. Over the 6-month period, the average air temperature was 15.2 °C, total precipitation was 502 mm, average relative humidity was 78.5%, average solar irradiance was 132.7 W m− 2, and average wind speed was 10.7 km h− 1. The plastic mulch films were laid onto rotavated 4 m x 1.2 m plots and secured by burying the edges at 10 cm soil depth. Plots were arranged in a 4-block design with random plot allocation for each mulch film type within each block, with 4 replicates per mulch film. Zea mays L. was grown to harvest through the two plastic mulch films with a seed density of 14 seeds m− 2 to simulate realistic mulch film use in an agricultural setting. A 10 cm x 10 cm exposed film sample was taken in monthly intervals from each plot, randomising sampling location within each plot. Mulch films were first laid out onto the field on 31st May 2022 and removed on 28th November 2022. For the artificial degradation, four laboratory methods were compared, and new, unexposed film samples were exposed for a duration of 20 weeks with weekly sampling intervals. The first method was heat exposure (oven-aging), using an 80 °C standard fan-oven (FED 400; Binder GmbH, Germany). LDPE and PLA/PBAT films were cut into 5 cm x 5 cm pieces (n = 100), placed into two separate glass beakers, and left in the oven. Film pieces in each beaker were mixed at each sampling point to prevent adhesion, and samples for analysis (n = 4) were selected randomly from each beaker and removed. The second method was UVA irradiance using a Suntest XXL + FD light stability test chamber (Atlas Material Testing Technology, Illinois, USA) with 3 × 1700 W xenon lamps with wavelength set to 300–400 nm and irradiance at 60 W m− 2, a chamber temperature of 25 °C, and relative humidity of maximum 50%. Due to the constant airflow in the chamber, individual film pieces could not be secured, therefore a 35 cm x 35 cm piece of each mulch film was placed into the test chamber and secured at the corners, with an average 40 cm distance from the light bulbs. At each sampling point, the mulch films were removed for spectral analysis, and afterwards a 5 cm x 5 cm piece of each film was removed for storage (n = 1) before placing the films back into the chamber. After an exposure time of 20 weeks, this equates to a UVA dose of 725.8 MJ m− 2. This method is more representative of natural weathering and involves deeper penetration of the UVA (in comparison to UVC) which might lead to bulk property changes. The third method was low UVC irradiance at an average of 1.6 W m− 2 (measured at wavelength range of 220–275 nm) using a LabGard Class II biosafety cabinet (NuAire Inc., Minnesota, USA) with a standard 30 W UVC lamp. Due to small chamber space, mulch films were cut into 5 cm x 5 cm pieces (n = 4) and placed centrally under the light bulb at 68 cm distance from the light source. Samples were removed at each sampling point for spectral analysis, then returned to the UVC cabinet with rotating positions to ensure even UV exposure of all samples. After an exposure time of 20 weeks, this equates to a UVC dose of 19.4 MJ m− 2. The higher energy of UVC is expected to cause more immediate surface interactions, leading to more surface concentrated degradation, less penetration depth, and more rapid surface modifications. Lastly, the fourth method was high UVC irradiance at an average of 3.9 W m− 2 (measured at wavelength range of 220–275 nm) using the same exposure method as described for low UVC irradiance, but with a 16 cm distance from the light source. After an exposure time of 20 weeks this equates to a UVC dose of 47.2 MJ m− 2. The exposure methods are from this point onwards referred to as field, heat, Suntest, low UVC, and high UVC exposure, respectively. Control spectra were taken from new, unexposed films, from here on referred to as control.

# Fieldwork and/or laboratory instrumentation
[CONDITIONAL - required for experiments where instruments used]

- Film thickness: Thickness gauge, Mututoyo, Japan

- Film surface roughness: Surftest SJ-210, Mututoyo, Japan

- Chemical spectra (FTIR): Cary 630 ATR-FTIR, Agilent

- DSC/TGA: TGA/DSC 1 STARe System (Mettler Toledo, USA)

- Heat exposure: Fan oven (FED 400, Binder, Gernamy)

- UVA exposure: Suntest XXL+FD light stability test chamber (Atlas Material testing Technology, USA)

- UVC exposure: LabGard Class II biosafety cabinet (NuAire Inc, USA)

# Calibration steps and values
[CONDITIONAL – required where instruments have been used]

All analyses have been carried out alongside regular blanks and internal standards applicable for each instrument.

# Quality control

Data was curated and missing values were replaced with n/a.

# Miscellaneous

Published paper: https://doi.org/10.1007/s10924-024-03481-5